## Slide 1
Fig. 1 Optical microscope photo which indicates the change in Si particle shape depending on time of solid solution treatment from 120 minutes to 480 minutes by fluidized bed furnace.
(a) 15 min
(b) 30 min
(c) 45 min
(d) 60 min
(e) 120 min
(f) 480 min
20 μm

## Slide 2
(a) 813 K
(b) 828 K
(c) 843 K
Fig. 2 Optical microscope photo which indicates the change in Si particle shape depending on temperature of solid solution treatment by fluidized bed furnace.
20 μm

## Slide 3
Vickers hardness, Hv
60
70
80
90
100
110
10-2
10-1
100
101
102
103
0 s
3 s
9 s
18 s
30 s
45 s
Aging time, t / ks
(a) Changes in hardness during aging
(b) Strength and ductility
50
220
240
260
280
0
10
20
30
40
RA
εf
sUTS
s0.2
0
1
2
3
4
sUTS, s0.2 / MPa
RA (%), εf
Time, t / s
Fig. 3 Effect of time delay between solid solution treatment and water cooling on mechanical properties in fluidized bed furnace.

## Slide 4
60
70
80
90
100
110
10-2
10-1
100
101
102
103
15 min
30 min
45 min
60 min
120 min
480 min
Vickers hardness, Hv
Aging time, t / ks
RA (%), εf
150
180
210
240
270
300
0.5
5
50
RA
εf
sUTS
s0.2
Time, t / ks
sUTS, s0.2 / MPa
0
1
2
3
4
(a) Changes in hardness during aging
(b) Strength and ductility
Fig. 4 Effect of solid-solution treatment time on mechanical properties in fluidized bed furnace.

## Slide 5
0
0.02
0.04
0.06
0.08
0.10
0
2
4
6
8
10
12
14
16
15
30
45
60
120
480
Average diameter
Volume fraction
Volume fraction, Vf (%)
Solution treatment time, t / min
Average diameter, d / μm
Fig. 5 Changes in size and volume fraction of pores during solid-solution treatment by fluidized bed furnace.

## Slide 6
Equivalent diameter, d / mm
0
10
20
30
40
15 min
30 min
45 min
60 min
120 min
480 min
10-1
100
101
102
103
Number density, ρp / mm-3
(a) Effect of solution treatment time
0
20
40
60
80
813 K
828 K
843 K
10-1
100
101
102
103
Number density, ρp / mm-3
Equivalent diameter, d / mm
(b) Effect of solution treatment temperature
Fig. 6 Effects of time and temperature on distribution of pore size in solid-solution treatment by fluidized bed furnace.

## Slide 7
180
220
260
300
813
828
843
0
1
2
3
RA
εf
sUTS
s0.2
sUTS, s0.2 / MPa
RA (%), εf
Temperature, T / K
Vickers hardness, Hv
60
70
80
90
100
110
10-2
10-1
100
101
102
103
813 K
828 K
843 K
Ternary eutectic T:824.4K
Binary eutectic T:836.5K
Aging time, t / ks
(b) strength and ductility
(a) Change in hardness during aging
Fig. 7 Effect of solid-solution treatment temperature on mechanical properties in fluidized bed furnace.

## Slide 8
y
(c) 843 K
12
Fig. 8 3D observation of pore properties depending on time of solid-solution treatment by fluidized bed furnace.
1.4 mm
1.4 mm
(a) 813 K
(b) 828 K
2.2 mm
x
z

## Slide 9
sUTS, s0.2 / MPa
60
70
80
90
100
110
10-2
10-1
100
101
102
103
Salt bath
(480 min)
Fluidized
bed furnace
(480 min)
Aging time, t / ks
Vickers hardness, Hv
(a) Change in hardness during aging
220
240
260
280
0
1
2
3
4
Salt bath
Fluidized
bed furnace
RA (%), εf
RA
εf
sUTS
s0.2
(b) Strength and ductility
Fig. 9 Comparison of mechanical properties in the sample that is heat-treated with fluidized bed furnace and mechanical properties in the sample that is heat-treated with salt-bath and oil-bath.

## Slide 10
Conditions | Ave. diameter (μm) | No. density (mm-3) | Sphericity (%) | Vol. fraction (%)
813 K - 60 min | 9.2 | 980 | 73.8 | 0.0465
828 K - 60 min | 9.0 | 236 | 74.8 | 0.0095
843 K - 60 min | 14.8 | 565 | 67.1 | 0.2847
12
Table 1 Effect of solid-solution treatment temperature on pore properties in fluidized bed furnace. Average diameter, number density, sphericity and volume fraction of pore obtained by quantitative analysis are listed.